## Slide 1: Making Sustainability Economic
Hobart, Tasmania, Australia where I live
I will have to race over some slides but the presentation is always downloadable from the net if you missed something.
All I ask is that you think about what I am saying.
John Harrison B.Sc. B.Ec. FCPA.
The Only Option that Will Deliver?

## Slide 2: Sustainability Requires a Holistic Approach
Our approach to sustainability and the most pressing problem of reducing CO2 in the air should be holistic and involve:
  Reductions in energy usage.
    Kyoto, energy rationing etc.
  Reductions in linkages to the environment
    Closing loops, recycling etc.
  Massive sequestration
    Geological sequestration, mineral sequestration and stopping de-afforestation.
Of the above massive sequestration is politically easiest to implement and could potentially be an economic process.
There is huge scope for sequestration and conversion of waste to resource in the built environment given the massive size of the materials flows involved.

## Slide 3: Economically Driven Sustainability
In the past it was considered that economic development was linked to.
  growth in use of resources and energy.
  Population growth.
We now understand that change itself is a stimulant for economic growth.
Consider the implications of changing to carbon compounds or materials containing carbon as building materials.
The challenge is to harness human behaviours which underlay economic supply and demand phenomena by changing the technical paradigm in favour of making carbon dioxide a resource.

## Slide 4: Achieving Sustainable Sustainability
Our goal should be:
  To make sustainability an economic process.
To do this we need to induce changes in demand and supply reducing energy and resource usage and detrimental linkages with the planet.
  Through education induce cultural change to increase the demand for sustainability.
  Innovate to change the technical paradigm to deliver sustainability.
TecEco tec, eco and enviro cements are innovative sustainability enabling technologies.

## Slide 5: Achieving Sustainability as an Economic Process
Increase in demand/price ratio for sustainability due to educationally induced cultural drift
#
$
Demand
Supply
Increase in supply/price ratio for more sustainable products due to innovative changes in the technical paradigm.
Equilibrium shift
Greater Sustainability and economic growth

## Slide 6: Techno Processes
Our linkages to the bio-geo-sphere are defined by techno processes describing and controlling the flow of matter and energy. It is these flows that have detrimental linkages to earth systems.
Detrimental affects on earth systems
The
technical
paradigm

## Slide 7: Earth Systems
Atmospheric composition, climate, land cover, marine ecosystems, pollution, coastal zones, freshwater systems, salinity and global biological diversity have all been substantially affected.

## Slide 8: There are Detrimental Affects Right Through the Techno Process
Take manipulate and make impacts
Greater Utility
End of lifecycle impacts
Less Utility
Linkages that affect earth system flows
Utility zone

## Slide 9: To Make Carbon a Resource the Key is To Change the Technology Paradigm
“By enabling us to make productive use of particular raw materials, technology determines what constitutes a physical resource1”
  Pilzer, Paul Zane, Unlimited Wealth, The Theory and Practice of Economic Alchemy, Crown Publishers Inc. New York.1990
To change the technical paradigm we must change both supply and demand, both of which feedback on each other in such a way as to move the equilibrium towards sustainability.

## Slide 10: We Must Re-Invent Many Materials
Take → Manipulate → Make → Use → Waste
[ ←Materials→]
What we take from the environment around us and how we manipulate and make materials out of what we take affects earth systems at both the take and waste ends of the techno-process.
The techno-process controls:
  How much and what we have to take to manufacture the materials we use.
  How long materials remain of utility and
  What form they are in when we eventually throw them “away”.
There is no such place as “away”, only a global commons

## Slide 11: Global Warming the Most Important Affect?
Trend of global annual surface temperature relative to 1951-1980 mean.

## Slide 12: Landfill – The Visible Legacy
Landfill is the technical term for filling large holes in the ground with waste. Landfills release methane, can cause ill health in the area, lead to the contamination of land, underground water, streams and coastal waters and give rise to various nuisances including increased traffic, noise, odours, smoke, dust, litter and pests.

## Slide 13: Our Linkages to the Environment Must be Reduced

## Slide 14: Fixing the Techno - Function
We need to change the techno function to:

## Slide 15: Fixing the Techno - Function
And more desirably to:
Recycling

## Slide 16: Recycling is Currently not Economic
Recycling is substantially undertaken for costly “feel good” political reasons and unfortunately not driven by sound economics
Making Recycling Economic Should be a Priority

## Slide 17: Recycling Materials = Reduced Emissions
The above relationships hold true on a macro scale, provided we can change the technology paradigm to make the process of recycling much more efficient = economic.

## Slide 18: Technical and Biological Complexity

## Slide 19: Recycling Can Involve Remixing
e.g Blending of waste streams may be required to produce input materials below toxicity levels of various heavy metals

## Slide 20: Materials - the Key to Sustainability
Materials are the key to our survival on the planet. The choice of materials controls emissions, lifetime and embodied energies, use of recycled wastes, maintenance of utility, recyclability and the properties of wastes returned to the bio-geo-sphere.

## Slide 21: Huge Potential for Sustainable Materials in the Built Environment
The built environment is made of materials and is our footprint on earth.
  It comprises buildings and infrastructure.
There are huge volumes involved. Building materials comprise
  70% of materials flows (buildings, infrastructure etc.)
  45% of waste that goes to landfill (15 % of new materials going to site are wasted.)
improving the sustainability of materials used to create the built environment will reduce the impact of the take and waste phases of the techno-process.
By including carbon, all materials are potentially carbon sinks.
All materials we make should not leave the techno-sphere
C
C
C
C
C
C
C

## Slide 22: The Largest Material Flow - Cement and Concrete
Concrete made with cement is the most widely used material on Earth accounting for some 30% of all materials flows on the planet and 60 - 70% of all materials flows in the built environment.
  Global Portland cement production is in the order of 2 billion tonnes per annum.
  Globally over 14 billion tonnes of concrete are poured per year.
  That’s over 2 tonnes per person per annum
TecEco Pty. Ltd. have benchmark technologies for improvement in sustainability and properties

## Slide 23: Embodied Energy of Building Materials
Downloaded from www.dbce.csiro.au/ind-serv/brochures/embodied/embodied.htm (last accessed 07 March 2000)
Concrete is relatively environmentally friendly and has a relatively low embodied energy

## Slide 24: Average Embodied Energy in Buildings
Downloaded from www.dbce.csiro.au/ind-serv/brochures/embodied/embodied.htm (last accessed 07 March 2000)
But because so much is used there is a huge opportunity for sustainability by reducing the embodied energy, reducing the carbon debt (net emissions) and improving properties.
Most of the embodied energy in the built environment is in concrete.

## Slide 25: Emissions from Cement Production
Portland cement used in construction is made from carbonate.
The process of calcination involves driving off chemically bound CO2 with heat.
CaCO3 →CaO + ↑CO2
∆
Heating also requires energy.
  Most energy is derived from fossil fuels.
  Fuel oil, coal and natural gas are directly or indirectly burned to produce the energy required releasing CO2.
The production of cement for concretes accounts for around 10%(1) of global anthropogenic CO2.
  (1) Pearce, F., "The Concrete Jungle Overheats", New Scientist, 19 July, No 2097, 1997 (page 14).

## Slide 26: Cement Production = Carbon Dioxide Emissions

## Slide 27: Innovative New Materials Vital
It is possible to achieve Kyoto targets as the UK are proving, but we need to go way beyond the treaty according to our chief scientists.
Carbon rationing has been proposed as the only viable means to keep the carbon dioxide concentration in the atmosphere below 450 ppm.
Atmospheric carbon reduction is essential, but difficult to politically achieve by rationing.
Making the built environment not only a repository for recyclable resources (referred to as waste) but a huge carbon sink is an alternative and adjunct that is politically viable as it potentially results in economic benefits.
Concrete, a cementitous composite, is the single biggest material flow on the planet with over 2.2 tonnes per person produced.
Eco-cements offer tremendous potential for capture and sequestration using cementitious composites.
MgCO3 → MgO + ↓CO2 - Efficient low temperature calcination & capture MgO + ↓CO2 + H2O → MgCO3.3H2O - Sequestration as building material ∆

## Slide 28: The Magnesium Thermodynamic Cycle

## Slide 29: Manufacture of Portland Cement

## Slide 30: TecEco Binders– A Blending System
TecEco concretes are a system of blending reactive magnesia, Portland cement and usually a pozzolan with other materials and are a key factor for sustainability.

## Slide 31: TecEco Formulations
Tec-cements (5-10% MgO, 90-95% OPC)
  contain more Portland cement than reactive magnesia. Reactive magnesia hydrates in the same rate order as Portland cement forming Brucite which uses up water reducing the voids:paste ratio, increasing density and possibly raising the short term pH.
  Reactions with pozzolans are more affective. After all the Portlandite has been consumed Brucite controls the long term pH which is lower and due to it’s low solubility, mobility and reactivity results in greater durability.
  Other benefits include improvements in density, strength and rheology, reduced permeability and shrinkage and the use of a wider range of aggregates many of which are potentially wastes without reaction problems.
Eco-cements (15-90% MgO, 85-10% OPC)
  contain more reactive magnesia than in tec-cements. Brucite in porous materials carbonates forming stronger fibrous mineral carbonates and therefore presenting huge opportunities for waste utilisation and sequestration.
Enviro-cements (15-90% MgO, 85-10% OPC)
  contain similar ratios of MgO and OPC to eco-cements but in non porous concretes brucite does not carbonate readily.
  Higher proportions of magnesia are most suited to toxic and hazardous waste immobilisation and when durability is required. Strength is not developed quickly nor to the same extent.

## Slide 32: Why Reactive Magnesia?
One of the most important variables in concretes affecting most properties is water.
  The addition of reactive magnesia has profound affects on both the fluid properties of water and the amount of water remaining in the mix during setting.
Corrosion texts describe the protective role of brucite.
  The consequences of putting brucite through the matrix of a concrete in the first place need to be considered.
Reactive MgO is a new tool to be understood with profound affects on most properties

## Slide 33: Sustainability
The Current Technical Driection
  Reduce the amount of total binder.
  Use more supplementary materials
    Pfa, gbfs, industrial pozzolans etc.
  Use of recycled aggregates.
    Including aggregates containing carbon
The use of MgO potentially overcomes:
  Problems using acids to etch plastics so they bond with concretes.
  Problem of sulphates from plasterboard etc. ending up in recycled construction materials.
  Problems with heavy metals and other contaminants.
  Problems with delayed reactivity e.g. ASR with glass cullet
Eco-cements further provide carbonation of the binder component.
Possibility of easy capture of CO2 during the manufacturing process.
Enhanced by using reactive MgO

## Slide 34: TecEco Kiln Technology
Grinds and calcines at the same time.
Runs 25% to 30% more efficiency.
Can be powered by solar energy or waste heat.
Brings mineral sequestration and geological sequestration together
Captures CO2 for bottling and sale to the oil industry (geological sequestration).
The products – CaO &/or MgO can be used to sequester more CO2 and then be re-calcined. This cycle can then be repeated.
Suitable for making reactive reactive MgO.

## Slide 35: Making Recycling Economic
Reducing, re-using and recycling is done more for feel good reasons than good economics and costs the community heaps!
To get over the laws of increasing returns and economies of scale and to make the sorting of wastes economic so that wastes become low cost inputs for the techno-process new technical paradigms are required. The way forward involves at least:
  A new killer technology in the form of a method for sorting wastes. (See TecEco web site for more details)
  A killer application for unsorted wastes.
TecEco cements are a low pH benign environment suitable for hosting many wastes

## Slide 36: A Killer Application for Waste?
Wastes
  Utilizing wastes based on their chemical composition involves energy consuming transport.
  Wastes could be utilized as resources depending on their class of properties rather than chemical composition.
    in vast quantities based on broadly defined properties such as light weight, tensile strength, insulating capacity, strength or thermal capacity in composites.
    Many wastes contain carbon and if utilized would result in net carbon sinks.
TecEco binders enable wastes to be converted to resources. Two examples:
  Plastics are currently hard to recycle because to be reused as manufacturing inputs they cannot usually be mixed. Yet they would impart light weight and insulating properties to a composite bound with the new carbon dioxide absorbing TecEco eco-cements.
  Sawdust and wood waste is burned in the bush contributing to global CO2. If taken to the tip, methane, which is worse is the end result. Yet wood waste it light in weight, has tensile strength, captured in a mineral binder is a carbon sink and provides excellent insulation.

## Slide 37: The Impact of TecEco Technology
TecEco magnesian cement technology will be pivotal in bringing about sustainability in the built environment.
  Tec-Cements Develop Significant Early Strength even with Added Supplementary Materials. Around 25 = 30% less binder is required for the same strength.
  Eco-cements carbonate sequestering CO2
  Both tec and eco=cements provide a benign low pH environment for hosting large quantities of waste
The CO2 released by calcined carbonates used to make binders can be captured using TecEco kiln technology.

## Slide 38: Our Dream - TecEco Cements for Sustainable Cities

## Slide 39: Robotics Will Result in Greater Sustainability
Construction in the future will be largely achieved using robots. Like a color printer different materials will be required for different parts of structures, and wastes such as plastics will provide many of the properties required for the cementitious composites used. A non-reactive binder such as TecEco tec-cements will supply the right rheology and environment, and as with a printer, there will be very little waste.

## Slide 40: TecEco Binders - Solving Waste Problems
An important objective should be to make cementitious composites that can utilise wastes.
TecEco cements provide a benign environment suitable for waste immobilisation.
Many wastes such as fly ash, sawdust , shredded plastics etc. can improve a property or properties of the cementitious composite.
There are huge materials flows in both wastes and building and construction. TecEco technology leads the world in the race to incorporate wastes in cementitous composites

## Slide 41: TecEco Binders - Solving Waste Problems (2)
If wastes are not immobile they should be immobilised.
TecEco cementitious composites represent a cost affective option for both use and immobilisation.
TecEco technology is more suitable than either lime, Portland cement or Portland cement lime mixes because of:
  Lower reactivity (less water, lower pH)
  Reduced solubility of heavy metals (lower pH)
  Greater durability
  Dense, impermeable and
  Homogenous.
  No bleed water
  Are not attacked by salts in ground or sea water
  Are dimensionally more stable with less cracking
TecEco cements are more predictable and easier to use than geopolymers.

## Slide 42: Why TecEco Binders are Excellent for Toxic and Hazardous Waste Immobilisation
In a Portland cement brucite matrix
  OPC takes up lead, some zinc and germanium
  Brucite and hydrotalcite are both excellent hosts for toxic and hazardous wastes.
  Heavy metals not taken up in the structure of Portland cement minerals or trapped within the brucite layers end up as hydroxides with minimal solubility.
The brucite in TecEco cements has a structure comprising electronically neutral layers and is able to accommodate a wide variety of extraneous substances between the layers and cations of similar size substituting for magnesium within the layers and is known to be very suitable for toxic and hazardous waste immobilisation.

## Slide 43: Lower Solubility of Metal Hydroxides
There is a 104 difference

## Slide 44: CO2 Abatement in Eco-Cements

## Slide 45: Embodied Energy and Emissions
Energy costs money and results in emissions and is the largest cost factor in the production of mineral binders.
  Whether more or less energy is required for the manufacture of reactive magnesia compared to Portland cement or lime depends on the stage in the utility adding process it is measured.
  Utility is greatest in the finished product which is concrete. The volume of built material is more relevant than the mass and is therefore more validly compared. On this basis the technology is far more sustainable than either the production of lime or Portland cement.
The new TecEco kiln technology will result in around 25% less energy being required and the capture of CO2 during production will result in less energy, lower costs and carbon credits.
The manufacture of reactive magnesia is a benign process that can be achieved with waste or intermittently available energy.

## Slide 46: Energy – On a Mass Basis
Relative to Raw Material Used to make Cement | From Manufacturing Process Energy Release 100% Efficient (MJ.tonne-1) | From Manufacturing Process Energy Release with Inefficiencies (MJ.tonne-1) | Relative Product Used in Cement | From Manufacturing Process Energy Release 100% Efficient (MJ.tonne-1) | From Manufacturing Process Energy Release with Inefficiencies (MJ.tonne-1) | Relative to Mineral Resulting in Cement | From Manufacturing Process Energy Release 100% Efficient (MJ.tonne-1) | From Manufacturing Process Energy Release with Inefficiencies (MJ.tonne-1)
CaCO3 + Clay | 1545.73 | 2828.69 | Portland Cement | 1807 | 3306.81 | Hydrated OPC | 1264.90 | 2314.77
CaCO3 | 1786.09 | 2679.14 |  |  |  | Ca(OH)2 | 2413.20 | 3619.80
MgCO3 | 1402.75 | 1753.44 | MgO | 2934.26 | 3667.82 | Mg(OH)2 | 2028.47 | 2535.59

## Slide 47: Energy – On a Volume Basis
Relative to Raw Material Used to make Cement | From Manufacturing Process Energy Release 100% Efficient (MJ.metre-3) | From Manufacturing Process Energy Release with Inefficiencies (MJ.metre-3) | Relative Product Used in Cement | From Manufacturing Process Energy Release 100% Efficient (MJ.metre-3) | From Manufacturing Process Energy Release with Inefficiencies (MJ.metre-3) | Relative to Mineral Resulting in Cement | From Manufacturing Process Energy Release 100% Efficient (MJ.metre-3) | From Manufacturing Process Energy Release with Inefficiencies (MJ.metre-3)
CaCO3 + Clay | 4188.93 | 7665.75 | Portland Cement | 5692.05 | 10416.45 | Hydrated OPC | 3389.93 | 6203.58
CaCO3 | 6286.62 | 8429.93 |  |  |  | Ca(OH)2 | 5381.44 | 8072.16
MgCO3 | 4278.39 | 5347.99 | MgO | 9389.63 | 11734.04 | Mg(OH)2 | 4838.32 | 6085.41

## Slide 48: Global Abatement
 | Without CO2 Capture during manufacture (billion tonnes) | With CO2 Capture during manufacture (billion tonnes)
Total Portland Cement Produced Globally | 1.80 | 1.80
Global mass of Concrete (assuming a proportion of 15 mass% cement) | 12.00 | 12.00
Global CO2 Emissions from Portland Cement | 3.60 | 3.60
Mass of Eco-Cement assuming an 80% Substitution in global concrete use | 9.60 | 9.60
Resulting Abatement of Portland Cement CO2 Emissions | 2.88 | 2.88
CO2 Emissions released by Eco-Cement | 2.59 | 1.34
Resulting Abatement of CO2 emissions by Substituting Eco-Cement | 0.29 | 1.53

## Slide 49: Abatement from Substitution
Figures are in millions of Tonnes
Building Material to be substituted | Realistic % Subst-itution by TecEco technology | Size of World Market (million tonnes | Substituted Mass (million tonnes) | CO2 Factors (1) | Emission From Material Before Substitution | Emission/Sequestration from Substituted Eco-Cement (Tonne for Tonne Substitution Assumed) |  | Net Abatement | 
 |  |  |  |  |  | Emissions - No Capture | Emissions - CO2 Capture | Abatement - No Capture | Abatement CO2 Capture
Bricks | 85% | 250 | 212.5 | 0.28 | 59.5 | 57.2 | 29.7 | 2.3 | 29.8
Steel | 25% | 840 | 210 | 2.38 | 499.8 | 56.6 | 29.4 | 443.2 | 470.4
Aluminium | 20% | 20.5 | 4.1 | 18.0 | 73.8 | 1.1 | 0.6 | 72.7 | 73.2
TOTAL |  |  | 426.6 | 20.7 | 633.1 | 114.9 | 59.7 | 518.2 | 573.4
Concretes already have low lifetime energies.
If embodied energies are improved could substitution mean greater market share?

## Slide 50: Sustainability Issues Summary
We will not kick the fossil fuel habit. It will kick us when we run out of fuel. Sequestration on a massive scales is therefore essential.
To reduce our linkages with the environment we must recycle.
Sequestration and recycling have to be economic processes or they have no hope of success.
We cannot stop progress, but we can change and historically economies thrive on change.
What can be changed is the technical paradigm. CO2 and wastes need to be redefined as resources.
New and better materials are required that utilize wastes including CO2 to create a wide range of materials suitable for use in our built environment.

## Slide 51: Policy Message Summary
Governments cannot easily legislate for sustainability, it is more important that ways are found to make sustainability good business.
  “Feel good” legislation does not work.
  EPR Legislation works but is difficult to implement successfully.
  Carbon rationing would be difficult to achieve globally.
It is therefore important for governments to make efforts to understand new technical paradigms that will change the techno-process so it delivers sustainable outcomes
Materials are the new frontier of technology
  Embedded intelligence enabling sorting should be globally standardized.
  Robotics are inevitable - we need to be prepared.
  Cementitious composites can redefine wastes as resources and sequester CO2.
  “The TecEco Technology Must be Developed” was a finding of the recent ISOS Conference. http://www.isosconference.org.au/entry.html

## Slide 52: Limiting Factors for Development of TecEco Technology
Credibility Issues that can only be overcome with significant funded research by TecEco and third parties.
Economies of scale
  Government procurement policies
  Subsidies for materials that can demonstrate clear sustainable advantages.
  Carbon taxes/credits.
Formula rather than performance based standards
  Formula based standards enshrine mediocrity and the status quo.
  A legislative framework enforcing performance based standards is essential.
  For example cement standards excluding magnesium are based on historical misinformation and lack of understanding.

## Slide 53: There is no End with TecEco Technology – Only a Beginning.
More technical slides follow

## Slide 54: TecEco Cements– A Blending System
TecEco cementitious composites are a system of blending reactive magnesia, Portland cement and usually a pozzolan with other materials.

## Slide 55: TecEco Formulations
Tec-cements (5-10% MgO, 90-95% OPC)
  contain more Portland cement than reactive magnesia. Reactive magnesia hydrates in the same rate order as Portland cement forming Brucite which uses up water reducing the voids:paste ratio, increasing density and possibly raising the short term pH.
  Reactions with pozzolans are more affective. After all the Portlandite has been consumed Brucite controls the long term pH which is lower and due to it’s low solubility, mobility and reactivity results in greater durability.
  Other benefits include improvements in density, strength and rheology, reduced permeability and shrinkage and the use of a wider range of aggregates many of which are potentially wastes without reaction problems.
Eco-cements (15-90% MgO, 85-10% OPC)
  contain more reactive magnesia than in tec-cements. Brucite in porous materials carbonates forming stronger fibrous mineral carbonates and therefore presenting huge opportunities for waste utilisation and sequestration.
Enviro-cements (15-90% MgO, 85-10% OPC)
  contain similar ratios of MgO and OPC to eco-cements but in non porous concretes brucite does not carbonate readily.
  Higher proportions of magnesia are most suited to toxic and hazardous waste immobilisation and when durability is required. Strength is not developed quickly nor to the same extent.

## Slide 56: Strength with Blend & Porosity
High OPC
High Magnesia
High Porosity
STRENGTH ON ARBITARY SCALE 1-100
Tec-cement concretes
Eco-cement concretes
Enviro-cement concretes

## Slide 57: Consequences of replacing Portlandite with Brucite
Portlandite (Ca(OH)2) is too soluble, mobile and reactive. It carbonates readily and being soluble can act as an electrolyte.
TecEco generally remove Portlandite using the pozzolanic reaction and add reactive magnesia which hydrates forming brucite which is another alkali, but much less soluble, mobile or reactive than Portlandite.
The consequences of removing Portlandite (Ca(OH)2 with the pozzolanic reaction and filling the voids between hydrating cement grains with Brucite Mg(OH)2, an insoluble alkaline mineral, need to be considered.

## Slide 58: TecEco Technology - Simple Yet Ingenious?
The TecEco technology demonstrates that magnesia, provided it is reactive rather than “dead burned” (or high density, periclase type), can be beneficially added to cements in excess of the amount of 5 mass% generally considered as the maximum allowable by standards
  Note that dead burned magnesia is much less expansive than dead burned lime (Ramachandran V. S., Concrete Science, Heydon & Son Ltd. 1981, p 358-360 )
Reactive magnesia is essentially amorphous magnesia with low lattice energy.
  It is produced at low temperatures and finely ground, and
  will completely hydrate in the same time order as the minerals contained in most hydraulic cements.
Dead burned magnesia and lime have high lattice energies
  Do not hydrate rapidly and
  cause dimensional distress.

## Slide 59: Summary of Reactions Involved
Notice the low solubility of brucite compared to Portlandite and that nesquehonite adopts a more ideal habit than calcite & aragonite
We think the reactions are relatively independent.

## Slide 60: Tec-Cements-Less Binder for the Same Strength.
Concretes are more often than not made to strength.
The use of tec-cement results in
  20-30% greater strength or less binder for the same strength.
  more rapid strength development even with added pozzolans.

## Slide 61: Reasons for Strength Development in Tec-Cements.
Reactive magnesia requires considerable water to hydrate resulting in:
  Denser, less permeable concrete.
  A significantly lower voids/paste ratio.
Higher early pH initiating more effective silicification reactions?
  The Ca(OH)2 normally lost in bleed water is used internally for reaction with pozzolans.
  Super saturation of alkalis caused by the removal of water?
Micro-structural strength due to particle packing (Magnesia particles at 4-5 micron are about 1/8th the size of cement grains.)
Slow release of water from around highly charged Mg++ ion?

## Slide 62: Water Reduction During the Plastic Phase
Water is required to plasticise concrete for placement, however once placed, the less water over the amount required for hydration the better. Magnesia consumes water as it hydrates producing solid material.
Less water results in less shrinkage and cracking and improved strength and durability. Concentration of alkalis and increased density result in greater strength.

## Slide 63: Tec-Cement Compressive Strength
Graphs by Oxford Uni Student

## Slide 64: Tec-Cement Tensile Strength
Graphs by Oxford Uni Student

## Slide 65: Other Strength Testing to Date
BRE (United Kingdom)
2.85PC/0.15MgO/3pfa(1 part) : 3 parts sand - Compressive strength of 69MPa at 90 days.
Note that there was as much pfa as Portland cement plus magnesia. Strength development was consistently greater than the OPC control
TecEco
The mix was:
Portland cement | 245 Kg | 10.88% | 12.29%
Magnesia | 30 Kg | 1.39% | 
Fly ash | 70 Kg | 3.24% | 
Quarry dust | 215 Kg | 9.55% | 
White sand | 550 Kg | 25.46% | 
Dolerate aggregate | 1060 Kg | 49.07% | 

## Slide 66: Tec-Cement Concrete Strength Gain Curve
The possibility of strength gain with less cement and added pozzolans is of great economic and environmental importance.

## Slide 67: A Few Warnings About Trying to Repeat TecEco Findings with Tec-Cements
MgO is a fine powder and like other fine powders has a high water demand so the tendency is to add too much water. As for other concretes this significantly negatively impacts on strength.
Mg++ when it goes into solution is a small atom with a high charge and tends to affect water molecules which are polar. The result is a Bingham plastic quality which means energy is required to introduce a shear thinning to allow placement.
Do not use the slump test!
  With ordinary Portland cement concretes as rheology prior to placement is observed in the barrel of a concrete truck whilst energy is applied by the revolving barrel.
  Is what is done in practice more accurate that the slump test anyway?

## Slide 68: Eco-Cement Strength Development
Eco-cements gain early strength from the hydration of OPC. Later strength comes from the carbonation of brucite forming an amorphous phase, lansfordite and nesquehonite.
Strength gain is mainly microstructural because of
  More ideal particle packing (Brucite particles at 4-5 micron are about 1/8th the size of cement grains.)
  The natural fibrous and acicular shape of magnesium carbonate minerals which tend to lock together.

## Slide 69: Eco-Cement Concrete Strength Gain Curve
Eco-cement bricks, blocks, pavers and mortars etc. take a while to come to the same or greater strength than OPC formulations but are stronger than lime based formulations.

## Slide 70: Eco-Cement Micro-Structural Strength

## Slide 71: Proof of Carbonation - Minerals Present After 18 Months
XRD showing carbonates and other minerals before removal of carbonates with HCl in a simple Mix (70 Kg PC, 70 Kg MgO, colouring oxide .5Kg, sand unwashed 1105 Kg)

## Slide 72: Proof of Carbonation - Minerals Present After 18 Months and Acid Leaching
XRD Showing minerals remaining after their removal with HCl in a simple mix (70 Kg PC, 70 Kg MgO, colouring oxide .5Kg, sand unwashed 1105 Kg)

## Slide 73: A Few Warnings About Trying to Repeat TecEco Findings with Eco-Cements
Eco-cements will only gain strength in materials that are sufficiently porous to allow the free entry of CO2.
Testing in accordance with standards designed for hydraulic cements is irrelevant.
There appears to be a paucity of standards that apply to carbonating lime mortars however we understand the European Lime project will rectify this.
Most knowledge of carbonating materials is to be found amongst the restoration fraternity.
Centuries of past experience and good science dictate well graded aggregates with a coarser fraction for sufficient porosity. These are generally found in concrete blocks made to today’s standards but not in mortars.

## Slide 74: Increased Density – Reduced Permeability
Concretes have a high percentage (around 18%) of voids.
On hydration magnesia expands 116.9 % filling voids and surrounding hydrating cement grains.
Brucite is 44.65 mass% water.
On carbonation to nesquehonite brucite expands 307%
Nesquehonite is 243.14% water and CO2
  Cheap binder!!!
Lower voids:paste ratios than water:binder ratios result in little or no bleed water less permeability and greater density.
  Compare the affect to that of vacuum dewatering.

## Slide 75: Reduced Permeability
As bleed water exits ordinary Portland cement concretes it creates an interconnected pore structure that remains in concrete allowing the entry of aggressive agents such as SO4--, Cl- and CO2
TecEco tec - cement concretes are a closed system. They do not bleed as excess water is consumed by the hydration of magnesia.
  As a result TecEco tec - cement concretes dry from within, are denser and less permeable and therefore stronger more durable and more waterproof. Cement powder is not lost near the surfaces. Tec-cements have a higher salt resistance and less corrosion of steel etc.

## Slide 76: Tec-Cement pH Curves
More affective pozzolanic reactions

## Slide 77: Eco-Cement pH Curves
More affective pozzolanic reactions

## Slide 78: A Lower More Stable Long Term pH
Eh-pH or Pourbaix Diagram The stability fields of hematite, magnetite and siderite
in aqueous solution; total dissolved carbonate = 10-2M.
In TecEco cements the long term pH is governed by the low solubility and carbonation rate of brucite and is much lower at around 10.5 -11, allowing a wider range of aggregates to be used, reducing problems such as AAR and etching. The pH is still high enough to keep Fe3O4 stable in reducing conditions.
Steel corrodes below 8.9

## Slide 79: Reduced Delayed Reactions
A wide range of delayed reactions can occur in Portland cement based concretes
  Delayed alkali silica and alkali carbonate reactions
  The delayed formation of ettringite and thaumasite
  Delayed hydration of minerals such as dead burned lime and magnesia.
Delayed reactions cause dimensional distress and possible failure.

## Slide 80: Reduced Delayed Reactions (2)
Delayed reactions do not appear to occur to the same extent in TecEco cements.
  A lower long term pH results in reduced reactivity after the plastic stage.
  Potentially reactive ions are trapped in the structure of brucite.
  Ordinary Portland cement concretes can take years to dry out however the reactive magnesia in Tec-cement concretes consumes unbound water from the pores inside concrete.
  Reactions do not occur without water.

## Slide 81: Carbonation
Carbonates are the stable phases of both calcium and magnesium.
Carbonation in the built environment would result in significant sequestration because of the shear volumes involved.
The formation of carbonates lowers the pH of concretes compromising the stability of the passive oxide coating on steel.
Carbonation adds considerable strength and some steel reinforced structural concrete could be replaced with fibre reinforced porous carbonated concrete.

## Slide 82: Carbonation (2)
There are a number of carbonates of magnesium. The main ones appear to be an amorphous phase, lansfordite and nesquehonite.
  Gor Brucite to nesquehonite = - 38.73 kJ.mol-1
  Compare to Gor Portlandite to calcite = -64.62 kJ.mol-1
The dehydration of nesquehonite to form magnesite is not favoured by simple thermodynamics but may occur in the long term under the right conditions.
Gor nesquehonite to magnesite = 8.56 kJ.mol-1
  But kinetically driven by desiccation during drying.
Reactive magnesia can carbonate in dry conditions – so keep bags sealed!
For a full discussion of the thermodynamics see our technical documents.
  TecEco technical documents on the web cover the important aspects of carbonation.

## Slide 83: Ramifications of Carbonation
Magesium Carbonates.
  The magnesium carbonates that form at the surface of tec – cement concretes expand significantly thereby sealing off further carbonation.
  Lansfordite and nesquehonite are formed in porous eco-cement concrete as there are no kinetic barriers. Lansfordite and nesquehonite are stronger and more acid resistant than calcite or aragonite.
  The curing of eco-cements in a moist - dry alternating environment seems to encourage carbonation via Lansfordite and nesquehonite .
  Carbonation results in a fall in pH.
Portland Cement Concretes
  Carbonation proceeds relatively rapidly at the surface. ?Vaterite? followed by Calcite is the principal product and lowers the pH to around 8.2

## Slide 84: Reduced Shrinkage
Dimensional change such as shrinkage results in cracking and reduced durability
Net shrinkage is reduced due to stoichiometric expansion of Magnesium minerals, and reduced water loss.

## Slide 85: Reduced Shrinkage – Less Cracking
After Richardson, Mark G. Fundamentals of Durable Reinforced Concrete Spon Press, 2002. page 212.
Cracking, the symptomatic result of shrinkage, is undesirable for many reasons, but mainly because it allows entry of gases and ions reducing durability. Cracking can be avoided only if the stress induced by the free shrinkage strain, reduced by creep, is at all times less than the tensile strength of the concrete. Tec-cements may also have greater tensile strength.
Reduced in TecEco tec-cements.

## Slide 86: Durability - Reduced Salt & Acid Attack
Brucite has always played a protective role during salt attack. Putting it in the matrix of concretes in the first place makes sense.
Brucite does not react with salts because it is a least 5 orders of magnitude less soluble, mobile or reactive.
  Ksp brucite = 1.8 X 10-11
  Ksp Portlandite = 5.5 X 10-6
TecEco cements are more acid resistant than Portland cement
  This is because of the relatively high acid resistance (?) of Lansfordite and nesquehonite compared to calcite or aragonite

## Slide 87: Improved Workability
Finely ground reactive magnesia acts as a plasticiser
There are also surface charge affects

## Slide 88: Bingham Plastic Rheology
The strongly positively charged small Mg++ atoms attract water which is polar in deep layers affecting the rheological properties.
It is not known how deep these layers get
Etc.
Etc.
Ca++ = 114, Mg++ = 86 picometres

## Slide 89: Rheology
TecEco concretes and mortars are:
  Very homogenous and do not segregate easily. They exhibit good adhesion and have a shear thinning property.
  Exhibit Bingham plastic qualities and react well to energy input.
  Have good workability.
TecEco concretes with the same water/binder ratio have a lower slump but greater plasticity and workability.
TecEco tec-cements are potentially suitable for mortars, renders, patch cements, colour coatings, pumpable and self compacting concretes.
  A range of pumpable composites with Bingham plastic properties will be required in the future as buildings will be “printed.”

## Slide 90: Robotics Will Result in Greater Sustainability
Construction in the future will be largely achieved using robots. Like a color printer different materials will be required for different parts of structures, and wastes such as plastics will provide many of the properties required for the cementitious composites used. A non-reactive binder such as TecEco tec-cements will supply the right rheology and environment, and as with a printer, there will be very little waste.

## Slide 91: Dimensionally Control Over Concretes During Curing?
Portland cement concretes shrink around .05%. Over the long term much more (>.1%).
  Mainly due to plastic and drying shrinkage.
The use of some wastes as aggregates causes shrinkage e.g. wood waste in masonry units, thin panels etc.
By varying the amount and form of magnesia added dimensional control can be achieved.

## Slide 92: Volume Changes on Hydration
When magnesia hydrates it expands:
MgO (s) + H2O (l) ↔ Mg(OH)2 (s)
40.31 + 18.0 ↔ 58.3 molar mass
11.2 + liquid ↔ 24.3 molar volumes
Up to 116.96% solidus expansion depending on whether the water is coming from stoichiometric mix water, bleed water or from outside the system. In practice much less as the water comes from mix and bleed water.
  The molar volume (L.mol-1)is equal to the molar mass (g.mol-1) divided by the density (g.L-1).

## Slide 93: Volume Changes on Carbonation
Consider what happens when Portlandite carbonates:
    Ca(OH)2 + CO2  CaCO3
    74.08 + 44.01 ↔ 100 molar mass
    33.22 + gas ↔ 36.93 molar volumes
  Slight expansion. But shrinkage from surface water loss
Compared to brucite forming nesquehonite as it carbonates:
    Mg(OH)2 + CO2  MgCO3.3H2O
    58.31 + 44.01 ↔ 138.32 molar mass
    24.29 + gas ↔ 74.77 molar volumes
  307 % expansion (less water volume reduction) and densification of the surface preventing further ingress of CO2 and carbonation. Self sealing?
  The molar volume (L.mol-1)is equal to the molar mass (g.mol-1) divided by the density (g.L-1).

## Slide 94: TecEco Cement Concretes –Dimensional Control
Combined – Hydration and Carbonation can be manipulated to be close to neutral.
  So far we have not observed shrinkage in TecEco tec - cement concretes (5% -10% substitution OPC) also containing fly ash.
  At some ratio, thought to be around 5% -10% reactive magnesia and 90 – 95% OPC volume changes cancel each other out.
  The water lost by Portland cement as it shrinks is used by the reactive magnesia as it hydrates eliminating shrinkage.
Note that brucite is 44.65 mass% water, nesquehonite is 243 mass% water and CO2
  It makes sense to make binders out of CO2 and water!.
More research is required for both tec - cements and eco-cements to accurately establish volume relationships.
  The molar volume (L.mol-1)is equal to the molar mass (g.mol-1) divided by the density (g.L-1).

## Slide 95: Tec - Cement Concretes – No Dimensional Change

## Slide 96: Reduced Steel Corrosion
Steel remains protected with a passive oxide coating of Fe3O4 above pH 8.9.
  A pH of over 8.9 is maintained by the equilibrium Mg(OH)2 ↔ Mg++ + 2OH- for much longer than the pH maintained by Ca(OH)2 because:
  Brucite does not react as readily as Portlandite resulting in reduced carbonation rates and reactions with salts.
Concrete with brucite in it is denser and carbonation is expansive, sealing the surface preventing further access by moisture, CO2 and salts.
Brucite is less soluble and traps salts as it forms resulting in less ionic transport to complete a circuit for electrolysis and less corrosion.
Free chlorides and sulfates originally in cement and aggregates are bound by magnesium
  Magnesium oxychlorides or oxysulfates are formed. ( Compatible phases in hydraulic binders that are stable provided the concrete is dense and water kept out.)

## Slide 97: Corrosion in Portland Cement Concretes
Passive Coating Fe3O4 intact
Both carbonation, which renders the passive iron oxide coating unstable or chloride attack (various theories) result in the formation of reaction products with a higher electrode potential resulting in anodes with the remaining passivated steel acting as a cathode.
Corrosion
Anode: Fe → Fe+++ 2e- Cathode: ½ O2 + H2O +2e- → 2(OH)- Fe++ + 2(OH)- → Fe(OH)2 + O2 → Fe2O3 and Fe2O3.H2O (iron oxide and hydrated iron oxide or rust)
The role of chloride in Corrosion
Anode: Fe → Fe+++ 2e- Cathode: ½ O2 + H2O +2e- → 2(OH)- Fe++ +2Cl- → FeCl2 FeCl2 + H2O + OH- → Fe(OH)2 + H+ + 2Cl- Fe(OH)2 + O2 → Fe2O3 and Fe2O3.H2O
Iron hydroxides react with oxygen to form rust. Note that the chloride is “recycled” in the reaction and not used up.

## Slide 98: Less Freeze - Thaw Problems
Denser concretes do not let water in.
Brucite will to a certain extent take up internal stresses
When magnesia hydrates it expands into the pores left around hydrating cement grains:
MgO (s) + H2O (l) ↔ Mg(OH)2 (s)
40.31 + 18.0 ↔ 58.3 molar mass
11.2 + 18.0 ↔ 24.3 molar volumes
39.20 ↔ 24.3 molar volumes
38% air voids are created in space that was occupied by magnesia and water!
Air entrainment can also be used as in conventional concretes
TecEco concretes are not attacked by the salts used on roads

## Slide 99: TecEco Binders - Solving Waste Problems
There are huge volumes of concrete produced annually ( 2 tonnes per person per year )
The goal should be to make cementitious composites that can utilise wastes.
TecEco cements provide a benign environment suitable for waste immobilisation
Many wastes such as fly ash, sawdust , shredded plastics etc. can improve a property or properties of the cementitious composite.
There are huge materials flows in both wastes and building and construction. TecEco technology will lead the world in the race to incorporate wastes in cementitous composites

## Slide 100: TecEco Binders - Solving Waste Problems (2)
If wastes are not immobile they should be immobilised.
TecEco cementitious composites represent a cost affective option for both use and immobilisation.
TecEco technology is more suitable than either lime, Portland cement or Portland cement lime mixes because of:
  Lower reactivity (less water, lower pH)
  Reduced solubility of heavy metals (lower pH)
  Greater durability
  Dense, impermeable and
  Homogenous.
  No bleed water
  Are not attacked by salts in ground or sea water
  Are dimensionally more stable with less cracking
TecEco cements are more predictable and easier to use than geopolymers.

## Slide 101: Role of Brucite in Immobilisation
In a Portland cement brucite matrix
  OPC takes up lead, some zinc and germanium
  Brucite and hydrotalcite are both excellent hosts for toxic and hazardous wastes.
  Heavy metals not taken up in the structure of Portland cement minerals or trapped within the brucite layers end up as hydroxides with minimal solubility.
The brucite in TecEco cements has a structure comprising electronically neutral layers and is able to accommodate a wide variety of extraneous substances between the layers and cations of similar size substituting for magnesium within the layers and is known to be very suitable for toxic and hazardous waste immobilisation.

## Slide 102: Lower Solubility of Metal Hydroxides
There is a 104 difference

## Slide 103: TecEco Materials are Fire Retardants
The main phase in TecEco tec - cement concretes is Brucite.
The main phases in TecEco eco-cements are Lansfordite and nesquehonite.
Brucite, Lansfordite and nesquehonite are excellent fire retardants and extinguishers.
At relatively low temperatures
  Brucite releases water and reverts to magnesium oxide.
  Lansfordite and nesquehonite releases CO2 and water and convert to magnesium oxide.
Fires are therefore not nearly as aggressive resulting in less damage to structures.
Damage to structures results in more human losses that direct fire hazards.

## Slide 104: High Performance-Lower Construction Costs
Less binders (OPC + magnesia) for the same strength.
Faster strength gain even with added pozzolans.
Elimination of shrinkage reducing associated costs.
Elimination of bleed water enables finishing of lower floors whilst upper floors still being poured and increases pumpability.
Cheaper binders as less energy required
Increased durability will result in lower costs/energies/emissions due to less frequent replacement.
Because reactive magnesia is also an excellent plasticiser, other costly additives are not required for this purpose.
A wider range of aggregates can be utilised without problems reducing transport and other costs/energies/emissions.

## Slide 105: TecEco Concretes - Lower Construction Costs (2)
Homogenous, do not segregate with pumping or work.
Easier placement and better finishing.
Reduced or eliminated carbon taxes.
Eco-cements can to a certain extent be recycled.
TecEco cements utilise wastes many of which improve properties.
Improvements in insulating capacity and other properties will result in greater utility.
Products utilising TecEco cements such as masonry and precast products can in most cases utilise conventional equipment and have superior properties.
A high proportion of brucite compared to Portlandite is water and of Lansfordite and nesquehonite compared to calcite is CO2.
  Every mass unit of TecEco cements therefore produces a greater volume of built environment than Portland and other calcium based cements. Less need therefore be used reducing costs/energy/emissions.

## Slide 106: TecEco Challenging the World
The TecEco technology is new and not yet fully characterised.
It offers sustainability in the built environment not previously considered possible.
The world desperately needs a way of sequestering large volumes of CO2 such as made possible by eco-cements.
Formula rather than performance based standards are preventing the development of new and better materials based on mineral binders.
TecEco challenge universities governments and construction authorities to quantify performance in comparison to ordinary Portland cement and other competing materials.
We at TecEco will do our best to assist.
Negotiations are underway in many countries to organise supplies to allow such scientific endeavour to proceed.

## Slide 107: TecEco’s Immediate Focus
TecEco will concentrate on:
  Killer applications that use a lot of cement, are easy to manage and that will initiate and achieve volume production.
  low technical risk products that require minimal research and development and for which performance based standards apply.
    Niche products for which our unique technology excels.
    Carbonated products such as bricks, blocks, stabilised earth blocks, pavers, roof tiles pavement and mortars that utilise large quantities of waste.
    Products where sustainability, rheology or fire retardation are required. (Mainly eco-cement technology using fly ash).
    Products such as oil well cement, gunnites, shotcrete, tile cements, colour renders and mortars where excellent rheology and bond strength are required.
  The immobilisation of wastes including toxic hazardous and other wastes because of the superior performance of the technology and the rapid growth of markets. (enviro and tec - cements).
  Controlled low strength materials e.g. mud bricks.
  Solving problems not adequately resolved using Portland cement
    Products where extreme durability is required (e.g.bridge decking.)
    Products for which weight is an issue.

## Slide 108: TecEco Minding the Future
TecEco are aware of the enormous weight of opinion necessary before standards can be changed globally for TecEco tec - cement concretes for general use.
  TecEco already have a number of institutions and universities around the world doing research.
TecEco have publicly released the eco-cement technology and received huge global publicity.
  TecEco research documents are available from the TecEco web site by download, however a password is required. Soon they will be able to be purchased from the web site. .
  Other documents by other researchers will be made available in a similar manner as they become available.
Technology standing on its own is not inherently good. It still matters whether it is operating from the right value system and whether it is properly available to all people.
-- William Jefferson Clinton

## Slide 109: A Few Other Comments
Research
  TecEco have found that in house research is difficult due to the high cost of equipment and lack of credibility of the results obtained.
  Although a large number of third party research projects have been initiated, the work has been slow due to inefficiencies and a lack of understanding of the technology. We are doing our best to address this with a new web site and a large number of papers and case histories that are being posted to it.
  TecEco are always keen to discuss research projects provided they are fair and the proposed test regime is appropriate.
Business
  There are significant business opportunities that are emerging particularly under the Clean Development Mechanism (CDM) of the Kyoto Protocol.
  TecEco are shifting the focus to tec-cement concretes due to economy of scale issues likely only to be overcome with the adoption of TecEco kiln technology and introduction of the superior Nichromet process (www.nichromet.com) to the processing of minerals containing Mg.
  Watch the development of robotic construction and placement without formwork as these new developments will require the use of binders with Bingham plastic qualities such as provided by TecEco technology.
  TecEco technology gives Mineral sequestration real economic relevance.

## Slide 110: Summary
Simple, smart and sustainable?
  TecEco cement technology has resulted in potential solutions to a number of problems with Portland and other cements including durability and corrosion, the alkali aggregate reaction problem and the immobilisation of many problem wastes and will provides a range of more sustainable building materials.
The right technology at the right time?
  TecEco cement technology addresses important triple bottom line issues solving major global problems with positive economic and social outcomes.
Climate Change | Pollution
Durability | Corrosion
Strength | Delayed Reactions
Placement , Finishing | Rheology
Shrinkage | Carbon Taxes

## Slide 111: Characteristics of TecEco Cements (1)
 | Portland Cement Concretes | Tec-Cement Concretes | Enviro-Cement Concretes | Eco-Cements
Typical Formulations | 100 mass% PC | 8 mass% OPC, 72 mass % PC, 20 mass% pozzolan | 20 mass% OPC, 60 mass % PC, 20 mass% pozzolan | 50 mass% OPC, 30 mass % PC, 20 mass% pozzolan
Setting | Main strength from hydration of calcium silicates. | Main strength is from hydration of calcium silicates. Magnesia hydrates forming brucite which has a protective role. | Magnesia hydrates forming brucite which protects and hosts wastes. Carbonation is not encouraged. | Magnesia hydrates forming brucite then carbonates forming Lansfordite and nesquehonite.
Suitability | Diverse | Diverse. Ready mix concrete with high durability | Toxic and hazardous waste immobilisation | Brick, block, pavers, mortars and renders.
Mineral Assemblage (in cement) | Tricalcium silicate, di calcium silicate, tricalcium aluminate and tetracalcium alumino ferrite. | Tricalcium silicate, di calcium silicate, tricalcium aluminate, tetracalcium alumino ferrite, reactive magnesia. |  | 

## Slide 112: Characteristics of TecEco Cements (2)
 | Portland Cement Concretes | Tec-Cement Concretes | Enviro-Cement Concretes | Eco-Cements
Final mineral Assemblage (in concrete) | Complex but including tricalcium silicate hydrate, di calcium silicate hydrate, ettringite, monosulfoaluminate, (tetracalcium alumino sulphate), tricalcium alumino ferrite hydrate, calcium hydroxide and calcium carbonate . | Complex but including tricalcium silicate hydrate, di calcium silicate hydrate, ettringite, monosulfoaluminate, (tetracalcium alumino sulphate), tricalcium alumino ferrite hydrate, calcium hydroxide, calcium carbonate, magnesium hydroxide and magnesium carbonates. |  | 
Strength | Variable. Mainly dependent on the water binder ratio and cement content. | Variable. Mainly dependent on the water binder ratio and cement content. Usually less total binder for the same strength development | Variable, usually lower strength because of high proportion of magnesia in mix. | Variable.

## Slide 113: Characteristics of TecEco Cements (3)
 | Portland Cement Concretes | Tec-Cement Concretes | Enviro-Cement Concretes | Eco-Cements
Rate of Strength Development | Variable. Addition of fly ash can reduce rate of strength development. | Variable. Addition of fly ash does not reduce rate of strength development. | Slow, due to huge proportion of magnesia | Variable, but usually slower as strength develops during carbonation process.
pH | Controlled by Na+ and K+ alkalis and Ca(OH)2 in the short term. In the longer term pH drops near the surface due to carbonation (formation of CaCO3) | Controlled by Na+ and K+ alkalis and Ca(OH)2 and high in the short term. Lower in the longer term and controlled by Mg(OH)2 and near the surface MgCO3 |  | High in the short term and controlled by Ca(OH)2. Lower in the longer term and controlled by MgCO3
Rheology | Plasticisers are required to make mixes workable. | Plasticisers are not necessary. Formulations are generally much more thixotropic. |  | Plasticisers are not necessary. Formulations are generally much more thixotropic and easier to use for block making.

## Slide 114: Characteristics of TecEco Cements (4)
 | Portland Cement Concretes | Tec-Cement Concretes | Enviro-Cement Concretes | Eco-Cements
Durability | Lack of durability is an issue with Portland cement concretes | Protected by brucite, are not attacked by salts, do not carbonate, are denser and less permeable and will last indefinitely. |  | Protected by brucite, are not attacked by salts, do not carbonate, are denser and will last indefinitely.
Density | Density is reduced by bleeding and evaporation of water. | Do not bleed - water is used up internally resulting in greater density |  | 
Permeability | Permeable pore structures are introduced by bleeding and evaporation of water. | Do not bleed - water is used up internally resulting in greater density and no interconnecting pore structures |  | 
Shrinkage | Shrink around .05 - .15 % | With appropriate blending can be made dimensionally neutral as internal consumption of water reduces shrinkage through loss of water and magnesium minerals are expansive. |  | 

## Slide 115: Characteristics of TecEco Cements (5)
 | Portland Cement Concretes | Tec-Cement Concretes | Enviro-Cement Concretes | Eco-Cements
Insulating Properties | Relatively low with high thermal conductivity around 1.44 W/mK | Depends on formulation but better insulation as brucite is a better insulator |  | Depends on formulation but better insulation as brucite is a better insulator and usually contains other insulating materials
Thermal Mass | High. Specific heat is .84 kJ/kgK | Depends on formulation but remains high | Depends on formulation but remains high | 
Embodied Energy (of concrete) | Low, 20 mpa 2.7 Gj.t-1, 30 mpa 3.9 Gj.t-1 (1) | Approx 15-30% lower due to less cement for same strength, lower process energy for making magnesia and high pozzolan content(2). | Lower depending on formulation(2). | Depends on formulation Even lower due to lower process energy for making magnesia and high pozzolan content(2).

## Slide 116: Characteristics of TecEco Cements (6)
 | Portland Cement Concretes | Tec-Cement Concretes | Enviro-Cement Concretes | Eco-Cements
Re-cyclability | Concrete can only be crushed and recycled as aggregate. | Can be crushed and recycled as aggregate. | Can be crushed and fines re-calcined to produce more magnesia or crushed and recycled as aggregate or both. | Can be crushed and fines re-calcined to produce more magnesia or crushed and recycled as aggregate or both.
Fire Retardant | Ca(OH)2 and CaCO3 break down at relatively high temperatures and cannot act as fire retardants | Mg(OH)2 is a fire retardant and releases H2O at relatively low temperatures. |  | Mg(OH)2 and MgCO3 are both fire retardants and release H2O or CO2 at relatively low temperatures.

## Slide 117: Characteristics of TecEco Cements (7)
 | Portland Cement Concretes | Tec-Cement Concretes | Enviro-Cement Concretes | Eco-Cements
Sustainability | A relatively low embodied energy and emissions relative to other building products. High volume results in significant emissions. | Less binder for the same strength and a high proportion of supplementary cementitous materials such as fly ash and gbfs. Can be formulated with more sustainable hydraulic cements such as high belite sulphoaluminate cements. A wider range of aggregates can be used. Greater durability. | A high proportion of supplementary cementitous materials such as fly ash and gbfs. Can be formulated with more sustainable hydraulic cements such as high belite sulphoaluminate cements. A wider range of aggregates can be used. Greater durability. | A high proportion of supplementary cementitous materials such as fly ash and gbfs. Carbonate in porous materials reabsorbing chemically released CO2 A wider range of aggregates can be used. Greater durability.
Carbon emissions | With 15 mass% PC in concrete .32 t.t-1 After carbonation approximately .299 t.t-1 | With 15 mass% PC in concrete approx.29 t.t-1 After carbonation approximately .26 t.t-1 Could be lower using supplementary cementitous materials and formulated with other low carbon cement blends. |  | With 11.25 mass % magnesia and 3.75 mass % PC in concrete .241 t.t-1 With capture CO2 and fly ash as low as .113 t.t-1